IV4020-RR

Anti UV Cold Lamination Film-Enviormentally Friendly

Description：

Film：	80 micron Anti-UV clear glossy film.

Adhesive：Transparent adhesive

Liner： Width：

120gsm Pure wooden pulp paper with one side PE and silicon coating;

1.06/1.27/1.37/1.52m

Features：

- Product can be used for two years, more effectively protect the basic pictures;

- Film is flatly laminated against basic pictures, promoting products' grade and performance;

- 2 years Anti-UV,  can avoid the yellowing appearance caused by ultraviolet radiation.

- Passed REACH (NO 1907/2006), RoSH2.0 certification, and complies with EU environmental protection requirements.

Application：

Lamination film mainly used for protecting basic pictures(Advertising printing pictures, Ground guidance signs, Indoor advertising printing pictures)

Technical Data：

Test Condition：Indoor temperature 23±2℃,Relative Humidity 50±5%.

Test tools like Aluminum plate, glass, steel plate are used for below testing .

| Test Items | units | Test method | Average value |
| --- | --- | --- | --- |

| Thickness PVC | Micron | GB/T6672-2001 | 80±10 |
| --- | --- | --- | --- |
| Weight-liner | g/m² | GB4669-1995 | 120±10 |
| Weight-finished product | g/m² | GB4669-1995 | 255±20 |
| Initial adhesive | N/25mm | FTM 9 | ≥11 |
| 24h，180°peel | N/25mm | FTM 1 | ≥13 |
| Dimensional stability MD | mm | FTM 14 | ≤1.0 |
| Dimensional stability CD | mm | FTM 14 | ≤0.6 |
| Tensile strength MD | N/25 mm | GB/T1040.1-2006 | ≥40 |
| Tensile strength CD | N/25 mm | GB/T1040.1-2006 | ≥35 |
| Service temperature range |  |  | -20～+70 |

- All technical data is subject to change without prior notice

Storage Condition：

All INFLEX products need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources.

Printing Environment：

Production environment: Production environment: temperature of 25 ± 5 °C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Begin the cold lamination and other operation after the image  is complete dry.

Application Environment：

Temperature of 25 ± 5 °C, relative humidity of 50%±10%, paste on clean ,smooth, even, dust-free substrate surface.

Quality Assurance condition：

Shelf life: 12 months, stored in original carton box, preferably use within six months.

Two years guarantee, since the date of production.

Important Remark：

- Information mentioned on technical data sheet is based upon tests we believe to be reliable. Environment humidity more than 70% in different districts will impact the printing result.

- This SAV product is with permanent glue and has the possibilities of adhesive residual on different substrates according to how long time the images passed on substrates , we suggest to use the vinyl from same batch to join the sheets.

Product Application：