IV4060

Ultra Transparent Film With Removable Adhesive

Description：

Film：	100micron; ultra-clear glossy PVC film

Adhesive：Clear removable adhesive

Liner： Width：

125 micron matte PET liner

1.27/1.52m

Features：

- The product is painted on one side, affixed to the glass and acrylic surface, with double-side visible effect.

- Excellent printability and handling; Good dimensional stability after application.

- Print antiskid PET as substrate.

Application：

- Applicable to Vehicle Wrapping Media, Billboards, indoor and outdoor advertising

- Suitable for various solvent ink, Eco-solvent ink and UV ink

Technical Data：

Test Condition：Indoor temperature 23±2℃,Relative Humidity 50±5%.

Test tools like Aluminum plate, glass, steel plate are used for below testing .

| Test Items | units | Test method | Average value |
| --- | --- | --- | --- |

| Thickness PVC | Micron | GB/T6672-2001 | 100±10 |
| --- | --- | --- | --- |
| Weight-liner | g/m² | GB4669-1995 | 175±10 |
| Weight-finished product | g/m² | GB4669-1995 | 350±20 |
| Initial adhesive | N/25mm | FTM 9 | ≥8 |
| 24h，180°peel | N/25mm | FTM 1 | ≥5 |
| Dimensional stability MD | mm | FTM 14 | ≤1.0 |
| Dimensional stability CD | mm | FTM 14 | ≤1.5 |
| Tensile strength MD | N/25 mm | GB/T1040.1-2006 | ≥40 |
| Tensile strength CD | N/25 mm | GB/T1040.1-2006 | ≥30 |
| Service temperature range |  |  | -20～+70 |

- All technical data is subject to change without prior notice

Storage Condition：

All INFLEX products need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources.

Printing Environment：

Temperature of 25 ± 5 °C, relative humidity of 50% ±10%, clean dust-free environment; Please move the product to the printing environment 24 hours before printing. Do printing test before use and ensure to remain enough edge margins when printing.

Application Environment：

Temperature of 25 ± 5 °C, relative humidity of 50%±10%, paste on clean ,smooth, even, dust-free substrate surface.

Quality Assurance condition：

Storage period: 18 months in original packaging;

Period of use: The screen has not been printed, and is valid for 3 years from the production date of the product. Complaints will not be accepted after the expiration date.

Important Remark：

All INFLEX material descriptions, technical information and application recommendations are based on typical test results that we believe to be credible. In different countries and regions, the inkjet printing effect will decrease when the ambient humidity is higher than 70%.

This product is a removable adhesive product that guarantees removable performance for three years for painted boards or smooth back stickers item. It is not recommended to splice products from different batches.

Product Application：